# ANTIFREEZE RED

### Antifreeze concentrate for radiators

Description

GEDOL ANTIFREEZE RED is a “very long life” antifreeze based on high purity monoethylene glycol and

organic corrosion inhibitors.

Customer benefits

GEDOL ANTIFREEZE RED Excellent protection against corrosion, erosion, and cavitation, for aluminium water pumps.

Heat transfer remains optimised: fully organic additives allow avoiding any formation of deposits and leave surfaces clean.

GEDOL ANTIFREEZE RED is entirely safe to use in all cast iron or aluminium engines and in

cooling systems containing aluminium or copper alloy radiators.

GEDOL ANTIFREEZE RED contains no silicates, phosphates, chromates, nitrites or

Boron

The coolant fluids obtained by diluting GEDOL ANTIFREEZE RED are also inert to elastomeric seals and paints

Applications

GEDOL ANTIFREEZE RED antifreeze, when mixed with an appropriate quantity of water, becomes a coolant fluid recommended for all internal combustion engines in cars and vans, trucks, construction machinery and agricultural tractors.

GEDOL ANTIFREEZE RED is diluted in demineralised water (< 8°F) to form a permanent coolant that can be used throughout the year

#### TABLE OF PROTECTION

| % volume of GEDOL ANTIFREEZE RED | Freezing Point, °C (temperature at which first crystals appear ) |
| --- | --- |
| 33%* | -20 °C |
| 40% | -26 °C |
| 50% | -37 °C |

It is recommended that at least 33% of the final solution should be ANTIFREEZE RED. Do not use in proportions above 70%

PERFORMANCES LEVELS                                           SPECIFICATIONS*

| Colour | Red |
| --- | --- |
| ASTM D 3306 – D 1384 – D 4340 | Specific gravity at 20 °C 1,13 |
| CUNA NC 956 – 16/2012 | Temperature at which crystal appear 50% dilution by volume) °C <-38 |
| VW/Audi /Seat/Skoda-TL 774 D/F | Boiling point (undiluted) °C > 170 |
| BS 6580 | PH, dilution 50% by vol. 8 |
| Scania | Alcalinity reserve >6,5 |
| Volvo No 260 |  |
| Deutz/MWM 0199-2091 |  |
| Ford ESE-M97B44—A/WSS M97B44.D |  |
| GM/OPEL 1940656 |  |
| MAN 248,324SNF,MAN B&W D36 5600 |  |
| MB 325.3 |  |
| CUMMINS 90T8-4 |  |
| DAF 74002 |  |
| JOHN DEERE H24B1&C1 |  |
| NATO S-759 |  |
| LEYLAND TRUCKS |  |
| JAGUAR |  |

*The values given in this specifications table are typical values for information purposes only.