# PERMANENT ANTIFREEZE

### Antifreeze concentrate for radiators

Description

GEDOL PERMANENT ANTIFREEZE  is a special type  monoethylene glycol totally free from nitrites, amines, phosphates (NAP Free) and long duration (Permanent), with anti-corrosion and anti-foam inhibitors.

Customer benefits

GEDOL PERMANENT ANTIFREEZE is a fluid antifreeze based on monoethylene glycol with the inhibitors to ensuring that, in relation to the percentage of use, an operability at low temperatures ensures an efficient protection against the various types of metals present in the cooling circuit from corrosion, prevents the formation of deposits and foam, is compatible with the plastics and elastomeric (gaskets, sleeves) with which it comes into contact.

Applications

GEDOL PERMANENT ANTIFREEZE, when mixed with an appropriate quantity of water, becomes a coolant fluid recommended for all internal combustion engines in cars and vans, trucks, construction machinery and agricultural tractors.

GEDOL PERMANENT ANTIFREEZE is diluted in demineralised water (< 8°F) to form a permanent coolant that can be used throughout the year

#### TABLE OF PROTECTION

| % volume of GEDOL ANTIFREEZE | Freezing Point, °C (temperature at which first crystals appear ) |
| --- | --- |
| 33%* | -20 °C |
| 40% | -26 °C |
| 50% | -37 °C |

It is recommended that at least 33% of the final solution should be  PERMANENT ANTIFREEZE . Do not use in proportions above 70%

PERFORMANCES LEVELS                                                                                           SPECIFICATIONS*

| ASTM D 3306 - D 1384- D 4340-D6210 Typ 1-FF | Colour Green blue |
| --- | --- |
| CUNA NC 956 – 16/2012 | Specific gravity at 20 °C 1,13 |
| VW/Audi/Seat/Skoda TL 774 C | Temperature at which crystal appear 50% dilution by volume) °C <-38 |
| BS 6580 | Boiling point (undiluted) °C > 170 |
| AFNOR NFR -15-601 | PH, dilution 50% by vol. 8 |
| SAE J1034 | Alcalinity reserve >11 |
| BMW N600 69.0 |  |
| CHRYSLER MS 7170 |  |
| FIAT 9.55523-IVECO 18-1830 |  |
| CAT 002/132 |  |
| MAN 324 Type NF |  |
| MB 325.0-325.2 |  |
| MTU MTL 5048 |  |
| OPEL-GM B 0400240/QL130100/OPEL GME L1301 |  |
| RENAULT 41-0-001 TYPE C |  |
| SAAB 6901599 |  |
| SCANIA TB 1451 |  |
| VOLVO 1286083 |  |
| E/L 1515B |  |
| NATO S-759 |  |

*The values given in this specifications table are typical values for information purposes only.